## Slide 1
Development of high-resolution InSb detectors at USD
Presented By
Mathbar Singh Raut
Dongming Mei
Sanjay Bhattarai
Hao Mei
(University of South Dakota )
Seminar
May 11, 2022
Supported By:
NSF OISE-1743790
PIRE GEMADARC Collaboration

## Slide 2
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Outline
02
Introduction and Motivation
Czochralski method
Ge crystal growth at USD
Indium Antimonide Crystal
    Introduction
    Comparison with Ge crystal
    Crystal growth parameters
    Crystal Characterization
InSb Crystal Growth Chalanges
    Purity and Stoichiometry
    Dislocation
    Dopant segregation
    Striation

## Slide 3
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
CZ method
03
CZ method achieves much lower around 500 EPD
Seed crystal ((100) Ge) is dipped into the molten Ge
Withdraw slowly, while maintaining the temperature of melt just above the melting point.
The rate of crystal pulling and temperature ( via power supply) of melt are adjusted to control the growth of the crystal
Depletion depth of planar detector
  where, is the applied bias voltage, N is the net impurity concentration in the crystal, is the charge of electron and is the dielectric constant of Ge.
Net Impurity Concentration should be for full depletion of a ~cm thick detector.
Dislocation density 300-10000
Homogenous Impurity concentration along the detector.

## Slide 4
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Melting
04
Power supply of 11 KW with a current of 104 A
Takes 2-2.5 hours to melt 3.5 Kg Ge (melting point 937.4)
Image: Simulation of our furnace by using CENOS induction heating software
Fig: Simulation results very close to real melting process
Time ( s )
Temperature ( C )

## Slide 5
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Crystal Growth at USD
05
Material preparation
  ZR ingots of concentration of are etched with etchant
  Dried with compressed nitrogen gas
Crucible cleaning
  Deep cleaned by same etchant
Image: Crystal growth facility at USD

## Slide 6
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Diameter Control
The diameter (D) of the crystal is given by
= Rate of change of weight
= Pull rate
= Crucible radius
= Density of solid Ge
= Density of liquid Ge
Chart: Position (mm)
| 0 | 5 | 10 | 15 | 20.5 | 25 | 30 | 35 | 40 | 41 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 78 | 85 | 90 | 95 | 97
Power(KW) | 8.64 | 8.64 | 8.64 | 8.64 | 8.62 | 8.6 | 8.58 | 8.56 | 8.54 | 8.72 | 8.74 | 8.74 | 8.8 | 8.8 | 8.8 | 8.8 | 8.8 | 8.8 | 9 | 9.2 | 9.4 | 9.6 | 9.8
Growth rate (gm/s) | 0 | 0.0045556 | 0.0061111 | 0.010311 | 0.010694 | 0.013889 | 0.0345 | 0.057694 | 0.13975 | 0.22917 | 0.29514 | 0.36111 | 0.4375 | 0.47917 | 0.45833 | 0.44444 | 0.43056 | 0.38194 | 0.45139 | 0.44444 | 0.41667 | 0.034722 | 0.027778
Chart: Position (mm)
| 0 | 5 | 10 | 15 | 20.5 | 25 | 30 | 35 | 40 | 41 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 78 | 85 | 90 | 95 | 97 | 99
Diameter(Theor.) | 0 | 0.97184 | 1.1256 | 1.4621 | 1.8835 | 2.1464 | 3.3829 | 4.3747 | 5.8086 | 7.7189 | 8.8946 | 9.9447 | 11.0468 | 11.6074 | 11.3303 | 11.1421 | 10.9508 | 10.256 | 11.2366 | 11.1421 | 10.7565 | 2.3938 | 2.0355
Diameter (Mesrd.) | 0 | 0.96 | 1.1 | 1.4 | 1.8 | 2.1 | 3.3 | 4 | 5.5 | 7.5 | 8.5 | 9.5 | 10 | 10 | 10 | 10 | 10 | 9.7 | 9.7 | 10.6 | 10.6 | 2.3 | 2
06

## Slide 7
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
InSb: an introduction
07
InSb is a zincblende III-V semiconductor widely used in infrared imaging and magnetic field sensing
Highly sensitive mid-wave infrared sensing (3-5 μm)
Inherently weaker bond strength, soft and high electron mobility
Dark-grey silvery metal pieces or powder
Above 500 0C, antimony and antimony oxide vapor liberate
Narrow bandgap of 0.17 eV at 300 K and 0.23 eV at 80 K
Chart: Band gap Vs Temperature
| 0.1 | 1 | 15 | 29 | 43 | 57 | 71 | 85 | 99 | 113 | 127 | 141 | 155 | 169 | 183 | 197 | 211 | 225 | 239 | 253 | 267 | 281 | 299
E_g | 0.24 | 0.24 | 0.23974 | 0.23905 | 0.23796 | 0.2365 | 0.2347 | 0.23259 | 0.23018 | 0.2275 | 0.22457 | 0.22139 | 0.21799 | 0.21438 | 0.21058 | 0.20659 | 0.20243 | 0.1981 | 0.19362 | 0.189 | 0.18423 | 0.17934 | 0.17287
Ref : Littler, C. L., D. G. Seller, Appl. Phys. Lett. 46,10 (1985) 986-988.
Breakdown Field = 1000 V
Mobility electrons 
Mobility Holes 
Diffusion coeff.(e) 
Diffusion coeff.(h) 
Thermal Velocity(e) =
Thermal velocity(h) 

## Slide 8
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Energy resolution
08
Efficiency per mole at least 9.3 times of Ge as photoelectric effect varies with Z5
Single event Compton scattering scales as Z, i.e. InSb would have Peak-to-Compton ratio 6 times better than Ge
  F  is Fano factor
   is the gamma energy
   is the average energy needed to form an electron-hole pair
scales with the band gap and Fano factor comparable to Ge  yields resolution for InSb better than that of Ge at least by factor of 2.
Peak-to-Compton ratio  12 times better than Ge.

## Slide 9
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
InSb crystal growth parameters
09
The chamber walls of the CZ growth system
 quartz tube of 7.0 cm diameter
An inner quartz tube of 5.0 cm diameter  to control temperature gradient
Graphite crucible used = 3.8 cm in diameter  mounted on third quartz tube
Growth atmosphere = hydrogen flux
Flux = 3.5 ltr/min
Pulling speed = 2.0 cm/hrs
Rotational speed = 20 rev/min
Heated about 1 hour to 700 0C to get melt
Image : Metallographic picture of an InSb ingot polycrystalline

## Slide 10
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
A few challenges
10
1. Problem of complete charge collection
Slow hole mobility is the potential source of problem
Resolution to be equal with Ge, requires > 10
Severe limitation on the size of high-quality detectors
2. Problem of compensation
  In Ge, mobilities differ only by factor of 2
  Drifting in reasonable amount of time
  Drifting in InSb is almost impossible
  Drifting n-type is necessary
  Smallest anion F- is many times larger than Li+
  Small band gap makes drifting at elevated temp. unfeasible
Factors to be controlled
Purity and stoichiometry
Dislocation density
Anisotropic dopant segregation
Growth striations

## Slide 11
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Purity and stoichiometry
11
Impact both crystal quality and electrical properties
Key factors to control purity and stoichiometry
  Feedstock purity
    Requires on the order of 5N to 7N purity
    Zone refining:
      Tellurium ( k = 0.9) making ZR very inefficient
  Melt stoichiometry
    Increased occurrence of twins
    Under normal growth conditions, a small window exists, effects negligible even when ratio deviates slightly from 1:1
    At any temperature > absolute zero, there exists a finite equilibrium concentration of point defects ( vacancies, antisites and self-interstitials)
    Point defects increase the configurational entropy which decreases the free energy of the crystal
    The deviation for InSb in the max. range of (0.5-1) indium excess

## Slide 12
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Purity and Stoichiometry
12
Sb evaporation rate
  High relative vapor pressure of Sb
  At the melting point of InSb ( 800 K ), indium and antimony have vapor pressures of torr
Precautions or control measures:
  Should be grown in limited timeframe
  Heating the furnace walls to prevent condensation
  Controlling gas pressure and flow rate in the chamber
  Avoiding overheating at initial meltdown
  Sb evaporation rate increases exponentially with T, so the temp. set-point should not be over shot
Figure: (a) Equilibrium phase diagram of InSb with (b) magnification of the α-InSb solidus line

## Slide 13
Mathbar Singh Raut
CoSSURF Materials Science
05/11/2022
Dislocation
13
Defect formation energy is much lower compared to Si and Ge
Edge or screw-type or both
Adversely affect charge transport within the materials
Produce dangling atomic bonds and strain fields that scatter and/or trap charge carriers
Effectively reduces the charge carrier mobility and lifetime
Creates higher resistance in detector junctions, poor signal to noise ratio, and inconsistent detector response
The first highly likely chance for dislocation formation occurs when the seed is dipped into the melt
Largest sources:
  Stress on the crystal from thermal gradients
  Impurities at the growth interface
Relatively poor thermal conductivity  outside of the crystal will cool faster creating thermal stress

## Slide 14
Mathbar Singh Raut CoSSURF Materials Science
05/11/2022
14
Thank you !
Questions ???