## Slide 1: Sense and Sensitivity
XinRan Liu
The University of Edinburgh
Confronting the radiological screening challenges for next-generation rare event detectors

## Slide 2
Overview
Current Landscape
1
2
3
Future Backgrounds Requirements
Current UK Assay Capabilities
4
R&D Upgrades

## Slide 3
Liquid Xenon Experiments
LUX
PANDAX-II
XENON1T
250 kg
(100 kg)
580 kg
(362 kg)
2,000 kg
(1,042 kg)
3.4x10-46 cm2
2.5x10-46 cm2
7.7x10-47 cm2
2013
2016
2017
2.6x10-48 cm2
1.4x10-48 cm2
2022 + 3 live years
2022 + 5 live years
LZ
XENONnT
7,000 kg
(5,600 kg)
5,900 kg
(4,000 kg)
Typical detector improvements:
Mass
Detector components
Detection and analysis methods
Improve background
PandaX – 4T
6 x10-48 cm2
202x + 5 live years
4,000 kg
(2,800 kg)

## Slide 4
Current Landscape

## Slide 5
NO unicorns in this magical forest
Maybe here?
Current Landscape

## Slide 7
Liquid Xenon Experiments
LUX
PANDAX-II
XENON1T
250 kg
(100 kg)
580 kg
(362 kg)
2,000 kg
(1,042 kg)
3.4x10-46 cm2
2.5x10-46 cm2
7.7x10-47 cm2
2013
2016
2017
2.6x10-48 cm2
1.4x10-48 cm2
2020 + 3 live years
2020 + 5 live years
LZ
XENONnT
7,000 kg
(5,600 kg)
5,900 kg
(4,000 kg)
Darwin/G3
1x10-49 cm2
2023 + 7 live years
50,000 kg
(40,000 kg)
Typical detector improvements:
Mass
Detector components
Detection and analysis methods
Improve background
PandaX – 4T
6 x10-48 cm2
2020 + 5 live years
4,000 kg
(2,800 kg)

## Slide 8
Detector recipe:
Neutrinoless Double Beta Decay

## Slide 9
The earth is unfortunately a radioactive planet and in the case of Dark Matter and , the ‘signature’ of each process are similar to that of natural radioactivity.
The Challenge

## Slide 10
The Challenge
Requirements for next generation dark matter and 0vbb experiments:
  Upgrade HPGE to reach < 10 μBq/kg levels
  Increase radon emanation throughput with greater sensitivity
  Improve surface alpha radioassay sensitivities
  Improve ICPMS sensitivity to < ppt/ppq levels
  Coordinated international efforts to cross calibrate existing facilities and continued improvements.
Golden rule: Everything is radioactive, quantify
panic level via screening.

## Slide 11
The Solution
Mass Spectrometry, NAA
Gamma-ray Spectroscopy
Radon Emanation
Optical Microscopy
Alpha detectors

## Slide 12
One Lab To Rule Them All
Boulby UnderGround Screening (BUGS) Facility
A jewel in the crown of the Boulby Underground Laboratory
Facility designed to become a centre of excellence for material assay and cleanliness
Class 1,000 cleanroom
Hugely important to G3 DM and 0vββ material selection
Nitrogen produced onsite, argon delivered weekly
Minimal Rn reduction required, ~2.5 Bq/m3 ambient

## Slide 13
Gamma-ray Spectroscopy
The ambitious programme to reboot and expand the UK underground screening facility launched in 2013.
2013
2016
Starts with refurbishment of the existing p-type coax – renamed Lunehead
In 2016 added 3 S-ULB detectors in purpose-built castles inside a new class 1k cleanroom.
In 2021 S-ULB SAGe well detector commissioned
2022

## Slide 14
Radon Removal System
A radon removal system was designed and built, capable of removing the radon from the carrier gas by up to 10 orders of magnitude depending on the gas.

## Slide 15
Germanium Detector Background
Belmont
160% (3.2kg) p-type
P. Scovell

## Slide 16
Germanium Detector Background
Belmont
160% (3.2kg) p-type
214Pb at 352 keV – 150x reduction
P. Scovell

## Slide 17
Germanium Detector Background
New S-ULB SAGe well performance.
Detector | Relative Efficiency or type | Count rate (/kg/day) |  |  |  | 
Detector | Relative Efficiency or type | 351 keV (214Pb) | 609 keV (214Bi) | 238 keV (212Pb) | 1461 keV (40K) | 2615 keV (208Tl)
Roseberry | BE6530 | 0.15(7) | 0.15(7) | 0.8(3) | 0.8(2) | 0.2(1)
Chaloner | BE5030 | 5(1) | 4(1) | 7(1) | 8.4(14) | 2.1(5)
Belmont | 160% | 0.7(2) | 0.4(1) | 0.13(6) | 1.0(2) | 0.3(1)
Merrybent | 100% | 2.5(3) | 1.8(3) | 0.3(1) | 1.9(3) | 0.8(2)
Lunehead | 100% | 5.6(5) | 4.7(4) | 8.3(5) | 9.1(6) | 2.0(3)
Lumpsey | SAGe-Well | 104(2) | 60(2) | 166(3) | 7.0(6) | 12(1)
1.1(7)
1.3(3)
1.1(7)
1.7(7)
0.7(2)
P. Scovell

## Slide 18
XIA UltraLo 1800 – Alphas
As of 2021, two XIA UltraLo-1800 surface alpha counters running at Boulby – Kettleness & Ormesby.
Installed liner to reduce detector backgrounds.
Factor three improvement compared to surface lab due to more cosmics which can mimic background events.
Surface: 1 mBq/m2 Bulk: 30 mBq/kg
Sample | Duration (hrs) | Alphas | Surface Area (cm2) | Emissivity (⍺/khr/cm2) | Activity (mBq/m2)
Background (SS Tray) | 168 | 342 | 1800 | 1.24 ± 0.07 | 6.88 ± 0.38
Background (PTFE Liner) | 168 | 103 | 1800 | 0.38 ± 0.04 | 2.12 ± 0.22
PNNL Copper | 168 | 13 | 707 | 0.13 ± 0.04 | <0.72 ± 0.22

## Slide 19
Electroforming Copper
STFC awarded funding for ‘scope, feasibility and costing’ study of establishing an electroplating facility in Boulby.
  Lead by NEWS-G and ECuME experience.
Survey ongoing to assess UK interest.
https://www.surveymonkey.co.uk/r/7JLT2DW
Still open and takes <2 minutes.
This is highly complementary to the BUGS facility and existing detectors.

## Slide 20
Boulby Radon Emanation System

## Slide 22
The Boulby Radon Facility - Sensitivity
Sensitivity based on the performance of the UCL system, but there are several upgrades.
  New detector has lower background - factor 4.
  New detector must use nitrogen instead of helium, demonstrated comparable detection efficiency.
  The new system is entirely constructed by swagelok with integrated external components.
Large Volumes of gas at ~ 5 μBq/m3
Radon Emanation ~ 100 μBq per sample

## Slide 23
Cold Radon Emanation Facility
The worlds first cryogenic radon emanation system.
2 emanation chambers available:
A 2.7 L chamber, operational at several fixed temperatures.
A 200 L chamber, which can be cooled and stabilised at temperatures down to ~77 K.
  Allows measurements of whole detector components.
  Enables studies of emanation rate as a function of temperature.
Goal: to deliver a world-leading sensitivity ~1 uBq/m3 to 222Rn emanated from materials at temperatures of *relevance to rare-event searches.
*e.g., LXe & LAr temperatures.
E. Perry
Emily Perry - Poster 3!

## Slide 24
ICPMS
Dedicated low-background facility at UCL inside a iso 6 cleanroom.
Fast: 1-2 samples/day
Sensitivity of 10 ppt for 238U & 232Th
Requires expertise in sample preparation.
J. Dobson

## Slide 25
Outlook
“Yesterday’s discovery is today’s calibration…”
(R. Feynman)
“… and tomorrow’s background”
(V. Telegdi)
We have started R&D programme.
We would like to establish BUGS as a center of excellence for screening and cleanliness and the UK as the world leader in material assay.
We need to develop new assay techniques
  Multi HPGE in coincidence
  Cold Radon Emanation
  Improved surface and bulk alpha sensitivity - new detectors
  Watch this space!

## Slide 26: Thank you for listening!
Any Questions?