## Slide 1
Dmitry Chernyak
on behalf of the nEXO collaboration
The University of Alabama
Radon daughter plate-out
as a background source in nEXO

## Slide 2
Motivation: Radon daughter background
      Radon daughters can deposit on the nEXO detector surfaces while they are exposed to air:
222Rn daughters attach to surfaces of nEXO materials → accumulation of 210Pb → growth of 210Po →
→ possible (α, n) reactions on low-Z nuclei → neutrons can create 137Xe and background events in the active LXe
Detector part | Area [m2] | 210Po activity
TPC vessel | 7.84 | 4.7 mBq/m2
SiPMs | 11.43 | 200 mBq/m2
Sapphire rods | 0.5 | 1.0 Bq/m2
Charge backing | 2.54 | 1.1 Bq/m2
Interposer | 11.43 | 218 mBq/m2
Inner cryostat liner | 40.72 | 2.4 Bq/m2
Monte Carlo studies were performed to quantify how much 210Po can be present on each component to contribute 0.063% to the background or less.
What are allowable air exposure durations?
We need to know the 210Pb activity growth rate

## Slide 3
Radon daughter attachment problem: Growth
 | ─ | deposition length [m]
 | ─ | radon progeny equilibrium factor
 | ─ | surface area [m2]
 | ─ | specific Rn activity [Bq/m3]
 | ─ | number of atoms
 | ─ | deposition time
 | ─ | mean lifetime
 | ─ | deposition length [m]
 | ─ | radon progeny equilibrium factor
 | ─ | surface area [m2]
 | ─ | specific Rn activity [Bq/m3]
 | ─ | number of atoms
 | ─ | deposition time
 | ─ | mean lifetime
The growth rates for 218Po, 214Pb, and 214Bi are
218Po rate of change proportional to number of 218Po atoms in air, not 222Rn
Every 214Bi decay creates a 210Pb atom. The rate of growth of the 210Pb surface activity is
Effective collection length
For long exposure times (more than 3 h, ):
Collection distances are obtained as the ratios of measurable activities, modulo the equilibrium factors

## Slide 4
Radon daughter attachment problem: Decay
After removing samples from contact with air, the decay rates for 218Po, 214Pb, and 214Bi are
Get the effective collection length by measuring the time dependence of 218Po and 214Po (daughter of 214Bi) α-particles
The solutions of these equations are

## Slide 5
Sample exposure
Samples were exposed to air in a basement lab with high 222Rn activity
Basement lab exposure:
      The following environmental parameters were monitored and recorded:
        Temperature
        Relative humidity
        Pressure
        Radon concentration
        Filtered airflow
        Airborne particle concentrations
        Sample surface charge
      Some parameters can be controlled to create specific conditions
Rn source exposure:
      Purge box with the high-activity PYLON RN-1025 222Rn source
      Radon activity can be controlled by nitrogen flow and exposure time
      Radon activity was calibrated using Durridge RAD7 detector

## Slide 6
Measurements
Samples were measured using ORTEC Alpha Mega alpha spectrometer with the ULTRA-AS low-background silicon detector
      GEANT4 simulation was used to estimate the detection efficiency for each sample
218Po
214Po
Sample | Basement | Rn source
Copper | 391 | 14
SiPM | 96 | 6
HDPE | 138 | 7
Teflon | 133 | 11
Nickel | 123 | —
Fused Silica | 76 | —
Carbon Fiber | 58 | —
Metallized Silica | 55 | —
Sapphire | 57 | —
Number of measurements

## Slide 7
Radon source results
Sample | Number of measurements | Average effective collection length [m]
Copper | 14 | 0.020 ± 0.008
SiPM | 6 | 0.028 ± 0.008
HDPE | 7 | 0.016 ± 0.006
Teflon | 11 | 0.016 ± 0.003
218Po
214Po
Standard deviations reported
      Use of the radon source verified the time fit
      Effective collection lengths are similar for all samples

## Slide 8
218Po
214Po
Basement lab conditions
Samples were exposed to the basement air in the following conditions:
Fan ON High and Low airflows have 400 and 50 times higher volume exchange rates than one at SNOLAB, respectively.
218Po detection of about 16 atoms
Measurements are essentially background free
Surface covered with paper tissue
Fan ON High: Tent closed, air exchanges 2.89 min-1
Fan ON Low: Tent closed, air exchanges 0.36 min-1
Fan OFF: Tent closed, air exchanges 0 min-1
Fan OFF: Tent opened, air exchanges 0 min-1
Surface biased using HV

## Slide 9
Detailed attachment results

## Slide 10
Basement lab results: Copper

## Slide 11
Basement lab results: SiPM and HDPE
SiPM
HDPE

## Slide 12
Basement lab results: Other materials
Sapphire
Carbon Fiber
Nickel
Metallized Silica
Fused Silica
Teflon

## Slide 13
Basement lab results: All materials
      No pronounced materials dependence observed for measured materials
      Average effective collection length is lower for higher air volume exchange rates
At a radon concentration of 135 Bq/m3 and an allowable 210Po activity of 4.7 mBq/m2 the allowed exposure time is 30.5 hours, assuming the 210Po activity equals that of 210Pb

## Slide 14
Basement lab results : Biased Copper
Attachment reduction can be achieved by biasing or covering with a Kimwipe (factor 1059 ± 250 reduction due to coverage observed at -1000 V biasing).

## Slide 15
Radon progeny activities and equilibrium factor
Equilibrium factor for 218Po was measured using Bladewerx Sabre BPM2 alpha/beta monitor

## Slide 16
Comparison of results with Jacobi model
Copper measurement results were compared with Jacobi model.
The idea behind the Jacobi model is straight forward: account for all disappearance mechanisms, assuming steady state.
According to the Jacobi deposition model Fan OFF conditions are closest to SNOLAB environment.
Our application of Jacobi model can’t predict effective collection lengths quantitatively, but only qualitatively.
Volume exchange rate, min-1 | Clean tent | Effective collection length [m] | Average effective collection length [m] | 218Po equilibrium factor [a.u.] |  | 
 |  | Jacobi model | Measured | Jacobi model |  | Measured
 |  |  |  | Diffusive attachment to surfaces | Tuned attachment velocity | 
2.89 | Closed | 0.0028 | 0.08 ± 0.04 | 0.071 | 0.047 | 0.012 ± 0.003
0.36 | Closed | 0.017 | 0.15 ± 0.08 | 0.36 | 0.15 | 0.062 ± 0.019
0.0 | Closed | 0.13 | 0.23 ± 0.07 | 0.84 | 0.83 | 0.34 ± 0.09
 | Opened | 0.18 | 0.32 ± 0.24 | 0.93 | 0.93 | 0.45 ± 0.11
0.0070 | SNOLAB | 0.17 | 0.37 ± 0.02 | 0.94 |  | 
Comparative Dosimetry of Radon in Mines and Homes. National Academies Press, 1991

## Slide 17
Summary
      210Po surface radioactivity can contribute to a background of the nEXO experiment through nuclear (α, n) reactions
      Radon daughters in the air are not in equilibrium. Equilibrium factors are subject to change, introducing additional variability of the attachment observables
      Attachment lengths observed in a lab were much larger than those in a small exposure box coupled with a radon source
      Effective collection length was found to not depend strongly on the measured material
      Current implementation of Jacobi model indicates that radon daughter equilibrium conditions at SNOLAB are closest to Fan OFF data at UA
      Attachment reduction can be achieved by biasing or covering material with a Kimwipe tissue

## Slide 18
nEXO Collaboration